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SAFETY
Synthetic web sling inspection checklist
The daily check of each nylon, polyester or polypropylene web sling before use, against the removal-from-service conditions in OSHA 1910.184(i)(9): acid or caustic burns, melting or charring, snags, punctures, tears or cuts, broken or worn stitches, and distorted fittings.
How often: Each day before use, and during use where service conditions warrant   ·   Who: Competent person designated by the employer   ·   About 5 min   ·   18 items
	Site or area
	
	Date and time
	

	Asset or line
	
	Completed by
	


Before you use it
1. OSHA 29 CFR 1910.184(d) requires each sling and all fastenings and attachments to be inspected for damage or defects each day before use by a competent person designated by the employer, with additional inspections during use where service conditions warrant. Damaged or defective slings are removed from service immediately.
1. Under 1910.184(i)(9), a synthetic web sling is removed from service immediately for acid or caustic burns; melting or charring of any part of the sling surface; snags, punctures, tears or cuts; broken or worn stitches; or distortion of fittings. A repaired sling is used only if a sling manufacturer or equivalent entity repaired it and proof tested it to twice the rated capacity, with the certificate retained, and slings repaired in a temporary manner are not used (1910.184(i)(8)).
1. Each sling is marked or coded with its rated capacities for each type of hitch and its web material (1910.184(i)(1)). Nylon slings are not used where acids or phenolics are present, and polyester or polypropylene slings, or slings with aluminum fittings, not where caustics are present (1910.184(i)(6)); polyester and nylon slings are not used above 180 °F, and polypropylene above 200 °F (1910.184(i)(7)). Add the sling manufacturer’s criteria.
Sling
	NO.
	ITEM
	RESULT
	NOTES

	1
	Scan the sling tag
	 Visited
	

	2
	Marking or code legible: rated capacity for each type of hitch and the web material
	 Pass     Fail     N/A
	

	3
	Sling identification as marked
	


	4
	Web material
	 Nylon     Polyester     Polypropylene
	


Webbing and stitching
	NO.
	ITEM
	RESULT
	NOTES

	5
	No acid or caustic burns
	 Pass     Fail     N/A
	

	6
	No melting or charring of any part of the sling surface
	 Pass     Fail     N/A
	

	7
	No snags, punctures, tears or cuts
	 Pass     Fail     N/A
	

	8
	Uniform thickness and width; selvage edges not split
	 Pass     Fail     N/A
	

	9
	No broken or worn stitches at the eyes or end fittings
	 Pass     Fail     N/A
	

	10
	No temporary repairs
	 Pass     Fail     N/A
	


Fittings
	NO.
	ITEM
	RESULT
	NOTES

	11
	Fittings not distorted
	 Pass     Fail     N/A
	

	12
	Fittings free of sharp edges that could damage the webbing
	 Pass     Fail     N/A
	


Conditions of use
	NO.
	ITEM
	RESULT
	NOTES

	13
	Chemicals in the work area suit the web material and fittings
	 Pass     Fail     N/A
	

	14
	Expected temperature at the load
Polyester and nylon slings: not above 180 °F. Polypropylene slings: not above 200 °F.
	____________  °F
Limit  ____________
	

	15
	Sharp edges of the load padded or protected
	 Pass     Fail     N/A
	


Result
	NO.
	ITEM
	RESULT
	NOTES

	16
	Result
	 Fit for use     Removed from service
	

	17
	Photo of any defect
	 Photo taken
	

	18
	Competent person
	Name  ______________________________
Signature  ______________________________
Date  ______________________________


Follow-up
For each failed check or reading out of limit: what was found, what was done, and the work order raised for it.
	NO.
	WHAT WAS FOUND
	ACTION OR WORK ORDER
	OWNER
	DUE

	
	
	
	
	

	
	
	
	
	

	
	
	
	
	

	
	
	
	
	


References
1. OSHA 29 CFR 1910.184, slings
Free to use and adapt. To run it on mobile, with checkpoint scans, readings checked against their limits as they are entered, and photos and signatures attached to the check, see vardian.io/templates/synthetic-web-sling-inspection-checklist.
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